H05V-K PVC电线                            HOOK-UP WIRE

| ●额定温度：70℃ ●额定电压：300V/500V ●参考标准： DIN0282-3 (VDE) ●导体使用单支或绞合0.05-1mm2镀锡或裸铜 ●PVC绝缘，符合ROHS环保标准 ●绝缘厚度均匀、易裁线、易剥皮 | ●Rated temperature：70℃ ●Rated voltage：300V/500V ●Reference standard：DIN0282-3 (VDE) ●Solid or stranded , tinned or bare copper conductor 0.05-1mm2 ●PVC insulation ,comply with ROHS environmental standard ●Uniform insulation thickness to ensure easy stripping and cutting |
| --- | --- |

●用于一般电子、电器设备内部连接线，            ●For general purpose internal wiring of appliance.,

电机变压器和灯具引出线                          electronic equipments lead wires of motors

■印字 MARKING

VDE     H05V-K  () mm2  70℃ 300/500V  CLEVER

■产品结构   CABLE CONSTRUCTION

| 型号 STYLE | 导体 CONDUCTOR |  |  | 绝缘 INSULATION |  | 包装长度 PACKAGING LENGTH |  | 最大导体电阻 MAX.COND. RESISTANCE （Ω/km,20℃,DC） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | mm2 | 线数/线径 No./mm | 外径 DIA. (mm) | 厚度 THICKNESS （mm） | 外径 O.D. (mm) | 英制 Ft/Coil | 公制 M/Coil |  |
| H05V-K | 0.50 | 20/0.18 | 0.95 | 0.70 | 2.30 | 1000 | 305 | 40.1 |
|  | 0.75 | 30/0.18 | 1.15 | 0.70 | 2.55 | 1000 | 305 | 26.7 |
|  | 1.00 | 40/0.18 | 1.30 | 0.70 | 2.70 | 1000 | 305 | 20.0 |

conductor tolerance 单支导体公差：+/-0.005mm, wire tolerance芯线外径公差：ＯＤ+/-0.10mm。

以上仅供参考，详细规格按双方确认规格书为准